**CITY OF BILOXI**

**SPECIAL PROVISION NO. 907-608-1 CODE: (SP)**

**DATE: 06/27/2017**

**SECTION 608 - CONCRETE SIDEWALKS**

# Subsection 608.02 - Materials

Delete the second paragraph of Subsection 608.02 and insert the following paragraph:

Concrete used for sidewalks shall be Class “B” (3000 psi) and meet the requirements of Section 804.

## Subsection 608.03.2 - Excavation and In-Grade Preparation

After the first paragraph of Subsection 608.03.2, add the following paragraph:

The material under sidewalks shall be compacted in 6 to 8 inch lifts to 95% density in accordance with ASTM D 1557.

**Subsection 608.03.4 - Handling, Measuring, Proportioning, and Mixing Materials**

Delete the first sentence of Subsection 608.03.4 and insert the following:

The method of handling, measuring, proportioning and mixing concrete materials shall conform to Section 804.

# Subsection 608.03.5 – Placing Concrete

After the last paragraph of Subsection 608.03.5, add the following paragraph:

Handicap ramps shall be placed at all street intersections where sidewalks are available on both sides of the street for pedestrian use. Handicap ramps shall be installed in accordance with the drawings and the latest edition of the American National Standard “Accessible and Usable Building and Facilities”.

# Subsection 608.03.6 - Joints

After the last paragraph of Subsection 608.03.6, add the following paragraph:

Expansion joints shall be installed at thirty-foot (30’) intervals and contraction joints provided at five-foot (5’) intervals.

# Subsection 608.03.7 - Protection and Curing

Delete the first paragraph of Subsection 608.03.7 and insert the following paragraph:

Concrete shall be protected and cured in accordance with the requirements of 501.03.20.1 or by other methods approved by the City Engineer or his authorized representative. Concrete shall be cured for at least 72 hours. During curing time all traffic, both pedestrian and vehicular, shall be kept off the concrete. The Contractor shall protect the work from damage until release of maintenance. All sections, which are damaged before release of maintenance, shall be removed and reconstructed by the Contractor without extra compensation.

# Subsection 608.05 - Basis of Payment

Delete the first paragraph of Subsection 608.05 and add the following:

Concrete sidewalks (including decorative sidewalks such as stamped-concrete, washed aggregate, stained concrete, etc.) will be paid for at the contract unit price per square yard, which shall be full compensation for completing the work. Decorative walks shall be paid for as Concrete Sidewalks (With or Without Reinforcement - All Types). No additional compensation will be provided for the replacement of decorative walks.

Delete pay items 608-A and 608-B and add the following:

907-608-A: Concrete Sidewalk (Without Reinforcement-All Types) - per square yard

907-608-B: Concrete Sidewalk (With Reinforcement-All Types) - per square yard