**CITY OF BILOXI**

**SPECIAL PROVISION NO. 907-609-1 CODE: (SP)**

**DATE: 06/29/2017**

**SECTION 609 - CONCRETE GUTTER, CURB, AND COMBINATION CURB AND**

**GUTTER**

# Subsection 609.02 - Materials

Add the following sentence to the end of the first paragraph of Subsection 609.02:

Concrete used for curb, gutter, rolled type curb and gutter and combination curb and gutter shall be Class “B” (3000 psi).

# Subsection 609.03.1 - Excavation and In-Grade Preparation

After the last paragraph of Subsection 609.03.1 add the following paragraph:

The material under all curb and gutter shall be compacted in 6 to 8 inch lifts to 95% density in accordance with ASTM D 1557.

# Subsection 609.03.2.4 - Sections and Joints

After the last paragraph of Subsection 609.03.2.4 add the following paragraph:

Expansion joints shall be installed at thirty foot (30’) intervals and contraction joints provided at ten foot (10’) intervals.

# Subsection 609.03.2.5 - Finishing

After the last paragraph of Subsection 609.03.2.5 add the following paragraph:

The Contractor shall mark the face of the curb with an "S" or "W" stamped into the wet concrete where the curb is finished over a sewer or water service. Also the curb shall be marked with a “V” where the curb(s) is adjacent to a water valve. The marking in the curb shall be legible. The letters shall be an overall height of 3 inches and shall be embedded into the concrete a minimum depth of one-half inch and a maximum depth of one inch. The stamping tool shall be subject to approval by the City Engineer or his authorized representative.

# Subsection 609.03.2.6 - Protection and Curing

Delete the first paragraph of Subsection 609.03.2.6 and insert the following paragraph:

Concrete shall be cured for at least 72 hours. Curing shall be as set out in 501.03.20.1 or by other methods approved by the City Engineer or his authorized representative.

# Subsection 609.04 - Method of Measurement

Delete the last sentence of the first paragraph of Subsection 609.04 and insert the following:

No deduction will be made for curb and gutter running the length of driveways.

Delete the last two paragraphs of Subsection 609.04 and add the following paragraphs:

Deduction in length will be made for drainage structures such as catch basins and inlets installed in the curbing.

Excavation, backfill, expansion joint material, curb stamping and other related miscellaneous items will not be measured for separate payment. The cost thereof shall be absorbed in the unit prices bid for other items.

# Subsection 609.05 - Basis of Payment

Following the phrase "Payment will be made under" add the following pay item number:

907-609-F: Rolled Type Concrete Curb and Gutter - per linear foot